# Aluminum Tube Bending Formula Reference

Reference for estimating minimum bend radii on aluminum tube. Applies to fully tooled radial draw bending with suitable forming lubricant.

## Basic Bending Formula

For tube material with elongation values above 9%, use the formula directly:

F  =  π / (4S)       where S = Minimum Spec. Elongation

For alloys with elongation below 9%, use the Bending Factor "F" from the table below (based on lowest elongation value per subgroup).

## Bending Factor "F" and Elongation Subgroups by Alloy

| Tube Alloy & Temper | Bending Factor "F" | Elongation Subgroup |
| --- | --- | --- |
| 1060-0, 1060-H112, 1100-0, 3003-0 | .0302 | 26 – 30% |
| 1100-0, 3003-0, 5052-0 | .0393 | 20 – 25% |
| 5052-0, 6061-0, 6061-T4, 6063-0, 6063-T4 | .0491 | 16 – 19% |
| 2219-T31, T35 & T3511; 5083-0; 5086-0; 5454-0; 5456-0; 6066-T4; 2014-T4; 2024-T3 | .0561 | 14 – 15% |
| 7075-0, 5083-H111, 5086-H111, 5454-H111, 5456-H111, 6063-T1, 2024-0, 2014-0, 2014-T4 | .0654 | 12 – 13% |
| 6061-T6, 6063-T6, 1100-H12, 3003-H12, 5052-H32, 3005-H25 | .0785 | 10 – 11% |
| 1100-H14, H16; 3003-H14, H16; 6063-T832; 5052-H34, H36; 3005-H28, H29, H294; 3003-H28, H294 | .0859 | 6 – 9% |
| 1100-H18, 3003-H18, 5052-H38 | .0927 | 2 – 5% |

## Formulae for Minimum Centerline Bend Radii

Based on fully tooled radial draw bender. Convert fractional dimensions to nearest 1/8".

| ROUND TUBE | SQUARE TUBE |
| --- | --- |
| R = (D² × F / t) + 0.785D | R = (E² × F / t) + S |

| R | Centerline radius |
| --- | --- |
| D | Tube outside diameter |
| t | Wall thickness |
| F | Bending factor (from table above) |
| S | Specified side dimension of square tube |
| E | Equivalent diameter = 4S / 3.14 |

## Important Limitations & Notes

- Above limitations are based on fully tooled radial draw bending equipment with suitable forming lubricant properly applied.

- If slight deformation can be tolerated in the bending zone, minimum centerline radius can be reduced by 1/4 tube diameter when inside forming mandrel is omitted.

- When press bending with fully supporting wing type tooling and/or compression bending using the follow block method, multiply values by 2.

- Minimum centerline radius must be not less than 3 × D. All other bending methods, multiply values by 2.5 or no less than 4 × D.

Template version 1.0 — Harco Estimating Workbook